# Alternative Extended-Release Minoxidil Formulations

# Alternative Extended-Release Minoxidil Formulations

# Alternative Extended-Release Minoxidil Formulations

## Patent Design-Around Strategy for Veradermics’ HPMC Matrix Claims

Prepared: February 2026 Updated: February 5, 2026 (8.5mg dose formulations) Purpose: Competitive product development - formulations designed to avoid Veradermics patent WO2024091572A1 / US12268688B2

## Executive Summary

Veradermics’ patent claims specifically cover HPMC-based (hydroxypropyl methylcellulose) matrix tablets for extended-release oral minoxidil. This document presents five alternative formulation approaches using fundamentally different release mechanisms that are likely outside their patent claims:

- Elementary Osmotic Pump (EOP) - Osmotic pressure-driven release

- Controlled Porosity Osmotic Pump (CPOP) - Porous membrane osmotic system

- Multi-Particulate Pellet System (MUPS) - Ethylcellulose-coated pellets in capsule

- Lipid Matrix Tablet - Glyceryl behenate/palmitostearate matrix

- Bi-Layer Push-Pull Osmotic Tablet - Two-compartment mechanical pump

## Target Product Profile

| Parameter | Target | Rationale |
| --- | --- | --- |
| Dose per unit | 8.5 mg | Matches Veradermics VDPHL01 clinical dose |
| Total daily dose | 17 mg (8.5 mg × 2) | Matches Veradermics BID regimen |
| Release duration | 10-12 hours | Covers 12-hour dosing interval |
| Target Cmax | 6-10 ng/mL | Matches Veradermics (~7-8 ng/mL); well below cardiac threshold (20 ng/mL) |
| Target Tmax | 2-4 hours | Delayed vs immediate release |
| Dosing frequency | Twice daily (q12h) | Matches Veradermics regimen |
| Hair growth threshold | >1.62 ng/mL | Minimum effective concentration for 10-12 hours |
| Cardiac activity threshold | <20 ng/mL | Must stay below to avoid CV side effects |

### Key PK Thresholds (from Veradermics clinical data)

| Threshold | Value | Significance |
| --- | --- | --- |
| Cardiac activity threshold | 20 ng/mL | Above this: tachycardia, hypotension risk |
| Ideal therapeutic range | 5-15 ng/mL | Efficacy without cardiac effects |
| Hair growth threshold | 1.62 ng/mL | Minimum for hair follicle stimulation |
| Veradermics VDPHL01 Cmax | ~7-8 ng/mL | Their actual achieved Cmax |
| IR minoxidil 5mg Cmax | ~22 ng/mL | Exceeds cardiac threshold |

## Minoxidil Physicochemical Properties

| Property | Value | Implication |
| --- | --- | --- |
| BCS Classification | Class II | Low solubility, high permeability |
| Aqueous solubility | ~2.2 mg/mL | May need solubility enhancement |
| Molecular weight | 209.25 g/mol | Small molecule, good diffusion |
| pKa | 4.6 | Weak base |
| LogP | 1.24 | Moderate lipophilicity |

## FORMULATION 1: Elementary Osmotic Pump Tablet (EOP)

### Mechanism

Osmotic pressure drives drug solution through laser-drilled orifice. Fundamentally different from HPMC matrix swelling/erosion - uses cellulose acetate semipermeable membrane with zero-order release kinetics.

### Core Tablet Composition (per tablet)

| Component | Amount (mg) | % w/w | Function |
| --- | --- | --- | --- |
| Minoxidil | 8.5 | 3.4% | Active ingredient |
| Sodium chloride | 100.0 | 40.0% | Osmotic agent (osmogent) |
| Mannitol | 62.5 | 25.0% | Osmotic agent + filler |
| Polyethylene oxide (MW 200K) | 50.0 | 20.0% | Suspending/swelling agent |
| Povidone K30 | 18.75 | 7.5% | Binder |
| Magnesium stearate | 5.0 | 2.0% | Lubricant |
| Colloidal silicon dioxide | 5.25 | 2.1% | Glidant |
| Total core weight | 250.0 | 100% |  |

### Semipermeable Membrane Coating

| Component | Amount | Function |
| --- | --- | --- |
| Cellulose acetate (398-10) | 85% of coating | Semipermeable membrane former |
| PEG 3350 | 15% of coating | Plasticizer/pore former |
| Coating weight gain | 8-10% | Controls water permeation rate |
| Orifice diameter | 0.5 mm | Laser-drilled delivery port |

### Manufacturing Process

- Wet granulate minoxidil + osmogents + binder using purified water

- Dry at 50°C to <2% moisture content

- Mill through 30-mesh screen

- Blend with lubricant/glidant for 5 minutes

- Direct compress into 9mm round biconvex tablets at 12 kN

- Spray coat with cellulose acetate/PEG solution (acetone:water 9:1) in perforated pan coater

- Laser drill single 0.5mm orifice on one face

### Expected Release Profile

- Lag time: 1-2 hours (membrane hydration)

- Zero-order release: 2-12 hours

- 85% release by 14 hours

### Key Patent Differentiation

- No HPMC in formulation

- Osmotic mechanism vs. gel diffusion/erosion

- Cellulose acetate membrane vs. HPMC matrix

- Requires laser-drilled orifice

## FORMULATION 2: Controlled Porosity Osmotic Pump (CPOP)

### Mechanism

Water-soluble pore formers (sorbitol) create microchannels in cellulose acetate membrane upon contact with GI fluids. No laser drilling required. Distinct from matrix systems.

### Core Tablet Composition (per tablet)

| Component | Amount (mg) | % w/w | Function |
| --- | --- | --- | --- |
| Minoxidil | 8.5 | 4.25% | Active ingredient |
| Fructose | 80.0 | 40.0% | Osmotic agent |
| Lactose monohydrate | 55.0 | 27.5% | Filler + osmotic agent |
| PEG 6000 | 30.0 | 15.0% | Solubilizer + osmogent |
| Croscarmellose sodium | 13.0 | 6.5% | Wicking agent |
| Povidone K29/32 | 7.5 | 3.75% | Binder |
| Magnesium stearate | 6.0 | 3.0% | Lubricant |
| Total core weight | 200.0 | 100% |  |

### Controlled Porosity Membrane

| Component | % of coating | Function |
| --- | --- | --- |
| Cellulose acetate (CA 320S) | 70% | Membrane former |
| Sorbitol | 20% | Water-soluble pore former |
| PEG 400 | 10% | Plasticizer |
| Coating weight gain | 6-8% |  |

### Manufacturing Process

- Blend all core components

- Wet granulate with PVP solution

- Dry and compress into 8mm tablets

- Prepare coating solution in acetone:methanol (8:2)

- Spray coat in fluidized bed coater

- No drilling required - pores form in situ

### Expected Release Profile

- Initial lag: 30-60 minutes

- Controlled release: 1-12 hours

- 90% release by 14 hours

### Key Patent Differentiation

- Porous membrane system vs. gel matrix

- No HPMC used

- In-situ pore formation vs. pre-formed matrix

- Osmotic driving force vs. concentration gradient

## FORMULATION 3: Multi-Particulate Pellet System (MUPS Capsule)

### Mechanism

Drug-loaded pellets with rate-controlling ethylcellulose/Eudragit polymer coating. Completely different architecture from monolithic matrix tablet. Drug release by diffusion through coating membrane.

### Pellet Core (drug-layered on sugar spheres)

| Component | Amount per capsule | Function |
| --- | --- | --- |
| Sugar spheres (25-30 mesh, 710-850 μm) | 255 mg | Inert core |
| Minoxidil | 8.5 mg | Active ingredient |
| HPMC E5 (binder solution) | 17 mg | Drug layering binder |
| Talc | 8.5 mg | Anti-tacking agent |

### Seal Coat (between drug layer and SR coating)

| Component | Function |
| --- | --- |
| HPMC E5 | Barrier layer |
| Weight gain | 2-3% |

### Sustained-Release Coating

| Component | % of coating | Function |
| --- | --- | --- |
| Ethylcellulose (Surelease® E-7-19040) | 60% | Rate-controlling polymer |
| Eudragit® RS 30D | 30% | Sustained release modifier (low permeability) |
| Triethyl citrate | 10% | Plasticizer |
| Coating weight gain | 18-22% | Controls release rate |

### Capsule Fill

- Fill ~290 mg coated pellets into Size 1 hard gelatin or HPMC capsule

- Option: Blend pellets with different coating levels (15%, 18%, 22%) for customized release profile

### Manufacturing Process

- Load sugar spheres into fluidized bed coater (Wurster insert)

- Apply drug layer solution (minoxidil + HPMC E5 in water:ethanol 7:3)

- Apply seal coat (HPMC E5 in water)

- Apply sustained-release coating (aqueous dispersion)

- Cure at 40°C/75% RH for 24 hours

- Fill into capsules

### Expected Release Profile

- 20-30% release at 2 hours

- 50-60% release at 6 hours

- 85% release at 12 hours

### Key Patent Differentiation

- Multi-particulate vs. monolithic tablet

- Ethylcellulose-based coating vs. HPMC matrix

- Capsule dosage form vs. tablet

- Diffusion through coating vs. gel erosion

- Reduced dose-dumping risk

- More predictable GI transit

### Advantages

- Flexible release profile (adjust coating level)

- Lower inter-subject variability

- Can combine with immediate-release pellets

- Well-established regulatory pathway

- Lowest dose-dumping risk at 8.5mg dose

## FORMULATION 4: Lipid Matrix Tablet (RECOMMENDED)

### Mechanism

Drug dispersed in waxy lipid matrix (glyceryl behenate/palmitostearate). Release by erosion and diffusion through hydrophobic lipid. Fundamentally different from hydrophilic HPMC gel matrix.

### Tablet Composition (per tablet) - OPTIMIZED FOR VERADERMICS-MATCHING PK

| Component | Amount (mg) | % w/w | Function |
| --- | --- | --- | --- |
| Minoxidil | 8.5 | 3.4% | Active ingredient |
| Compritol® 888 ATO (glyceryl behenate) | 112.5 | 45.0% | Lipid matrix former (increased for lower Cmax) |
| Precirol® ATO 5 (glyceryl palmitostearate) | 30.0 | 12.0% | Secondary lipid |
| PEG 6000 | 12.5 | 5.0% | Pore former (reduced for slower release) |
| Microcrystalline cellulose (Avicel PH-102) | 55.0 | 22.0% | Filler/compressibility aid |
| Lactose monohydrate | 17.5 | 7.0% | Filler |
| Poloxamer 188 | 3.75 | 1.5% | Surfactant (wetting) |
| Colloidal silicon dioxide (Aerosil 200) | 5.0 | 2.0% | Glidant |
| Magnesium stearate | 5.25 | 2.1% | Lubricant |
| Total tablet weight | 250.0 | 100% |  |

Total lipid content: 57% (optimized for Cmax ~6-10 ng/mL to match Veradermics)

### Manufacturing Process (Melt Granulation)

- Preheat mixer to 75-80°C

- Add Compritol + Precirol, allow to melt completely

- Add minoxidil, mix until dissolved/dispersed (5 min)

- Add MCC and lactose, mix thoroughly (10 min)

- Cool to room temperature while mixing

- Mill solidified mass through 20-mesh screen

- Blend with colloidal silica and magnesium stearate (3 min)

- Direct compress into 9mm tablets at 12 kN

### Alternative: Hot Melt Extrusion

- Premix minoxidil with lipids

- Extrude at 70-75°C through twin-screw extruder

- Mill extrudate to granules

- Blend and compress

### Expected Release Profile (Target for Cmax ~6-10 ng/mL)

- Near zero-order release kinetics

- 15-20% release at 1 hour (reduced initial burst)

- 40-50% release at 4 hours

- 65-75% release at 8 hours

- >80% release at 12 hours

- Maintain plasma levels >1.62 ng/mL (hair growth threshold) for 10-12 hours

### Key Patent Differentiation

- Lipid-based vs. hydrophilic polymer matrix

- Hydrophobic matrix vs. hydrophilic gel

- Drug release via lipid erosion + diffusion

- pH-independent release (lipids insoluble at all pH)

- No polymers used in matrix (only lipid excipients)

### Advantages

- Simple manufacturing (melt granulation)

- pH-independent release

- Good stability

- Low cost excipients

### Caution

- Potential food effect with high-fat meals (monitor in PK studies)

## FORMULATION 5: Bi-Layer Push-Pull Osmotic Tablet

### Mechanism

Two-compartment system with osmotic “push” layer that expands and drives drug from “pull” layer through laser-drilled orifice. Mechanical pumping action.

### Drug Layer (Pull Layer) - 120 mg

| Component | Amount (mg) | % w/w | Function |
| --- | --- | --- | --- |
| Minoxidil | 8.5 | 7.1% | Active ingredient |
| PEG 400 | 12.0 | 10.0% | Solubility enhancer |
| Sodium chloride | 36.0 | 30.0% | Osmogent |
| Polyethylene oxide (MW 100K) | 52.5 | 43.75% | Drug carrier/suspending agent |
| Povidone K30 | 11.0 | 9.15% | Binder |
| Total drug layer | 120.0 | 100% |  |

### Push Layer - 100 mg

| Component | Amount (mg) | % w/w | Function |
| --- | --- | --- | --- |
| Polyethylene oxide (MW 7M) | 60.0 | 60.0% | High MW expanding polymer |
| Sodium chloride | 25.0 | 25.0% | Osmogent |
| Ferric oxide (red) | 5.0 | 5.0% | Colorant/layer identifier |
| Hydroxypropyl cellulose (Klucel EF) | 10.0 | 10.0% | Binder |
| Total push layer | 100.0 | 100% |  |

### Membrane Coating

| Component | % of coating | Function |
| --- | --- | --- |
| Cellulose acetate | 80% | Semipermeable membrane |
| PEG 3350 | 20% | Plasticizer |
| Weight gain | 8% |  |

### Assembly

- Compress drug layer first

- Add push layer on top, compress bi-layer tablet

- Total tablet: 220 mg, 9mm caplet shape

- Coat with cellulose acetate membrane

- Laser drill single 0.4 mm orifice on drug layer side

### Manufacturing Process

- Prepare drug layer granulation (wet granulate, dry, mill)

- Prepare push layer granulation separately

- Fill drug layer into die, pre-compress lightly

- Add push layer, final compression

- Spray coat bi-layer tablets

- Laser drill orifice (positioned on drug layer face)

### Expected Release Profile

- Lag time: 1-2 hours

- Zero-order release: 2-14 hours

- 90% release by 16 hours

### Key Patent Differentiation

- Bi-compartment vs. single-layer matrix

- Mechanical pumping action vs. passive diffusion

- Uses polyethylene oxide, not HPMC

- Osmotic pressure drives release, not concentration gradient

## Comparative Analysis

| Feature | Veradermics (HPMC Matrix) | EOP | CPOP | MUPS | Lipid Matrix | Push-Pull |
| --- | --- | --- | --- | --- | --- | --- |
| Dose | 8.5 mg | 8.5 mg | 8.5 mg | 8.5 mg | 8.5 mg | 8.5 mg |
| Primary polymer/excipient | HPMC K4M/K200M | Cellulose acetate | Cellulose acetate | Ethylcellulose | Compritol/Precirol | PEO/Cellulose acetate |
| Release mechanism | Gel diffusion/erosion | Osmotic pump | Osmotic (porous membrane) | Coating diffusion | Lipid erosion | Osmotic push-pull |
| Dosage form | Monolithic tablet | Coated tablet | Coated tablet | Capsule with pellets | Monolithic tablet | Bi-layer tablet |
| Tablet/capsule weight | ~150-200 mg | 250 mg | 200 mg | ~290 mg (Size 1 cap) | 250 mg | 220 mg |
| Orifice required | No | Yes (laser) | No | No | No | Yes (laser) |
| pH dependency | Some | Minimal | Minimal | Minimal | None | Minimal |
| Food effect risk | Low | Low | Low | Low | Moderate | Low |
| Dose-dumping risk | Moderate | Low | Low | Lowest | Moderate | Low |
| Manufacturing complexity | Low | High | Medium | Medium | Low-Medium | High |
| Equipment needs | Standard | Laser drill | Standard coating | Wurster coater | Melt granulator | Laser drill |
| Regulatory precedent | Common | OROS products | Less common | Common (generic ER) | Moderate | OROS products |

## Recommended Development Priority

### First Choice: FORMULATION 3 (Multi-Particulate/MUPS)

Rationale: 1. Lowest dose-dumping risk - critical at 8.5mg where dose-dump could cause cardiac effects 2. Most established regulatory pathway for ER generics 3. No specialized equipment (laser drilling) required 4. Ethylcellulose coatings are well-characterized and approved 5. Flexible release profile customization by adjusting coating level 6. Lower manufacturing complexity than osmotic systems 7. Clear differentiation from HPMC matrix claims

### Second Choice: FORMULATION 4 (Lipid Matrix)

Rationale: 1. Simpler manufacturing (melt granulation or hot melt extrusion) 2. Completely different chemistry (lipids vs. polymers) 3. Very strong patent differentiation argument 4. pH-independent release 5. Low-cost, readily available excipients 6. Good stability profile 7. Caution: Monitor for food effects in PK studies

### Third Choice: FORMULATION 2 (CPOP)

Rationale: 1. Osmotic mechanism clearly different from matrix 2. No laser drilling required (unlike EOP) 3. Zero-order release kinetics 4. Food-independent absorption

## Development Considerations

### First-in-Human Study Design (8.5mg dose)

Recommended approach: 1. Dose escalation: Start with 2.5mg, then 5mg, then 8.5mg 2. Safety monitoring: Continuous ECG, BP every 30 min for first 4 hours 3. PK sampling: Pre-dose, 0.5, 1, 2, 3, 4, 6, 8, 10, 12, 14, 16, 24 hours 4. Food effect arm: Compare fasted vs. high-fat meal (especially for lipid matrix)

### Bioequivalence Strategy

- Different release mechanisms may yield different PK profiles

- May need to target similar AUC rather than identical Cmax/Tmax

- Consider 505(b)(2) pathway if not bioequivalent to Veradermics product

### Stability Studies Required

- Accelerated stability (40°C/75% RH, 6 months)

- Long-term stability (25°C/60% RH, 12-36 months)

- Photostability (ICH Q1B)

- Minoxidil compatibility with each matrix type

### Scale-Up Considerations

- MUPS: Wurster coating equipment availability

- Lipid matrix: Melt granulation or HME equipment

- Osmotic systems: Laser drilling equipment, membrane coating expertise

### Regulatory Pathway Options

- 505(b)(2) - Reference Veradermics’ safety/efficacy data, own PK studies

- 505(j) ANDA - If bioequivalent, but need to design around patents

- New NDA - If claiming superiority or different indication

## Patent Validity Analysis: Critical Issue with Veradermics Claims

### The Problem: Claimed PK Parameters Overlap with Immediate-Release Minoxidil

Veradermics’ patent claims (US12268688B2) are written as METHOD claims covering any “modified release pharmaceutical formulation” achieving specific pharmacokinetic parameters:

| Claim Element | Veradermics Patent Claims |
| --- | --- |
| Dose range | 3.5 - 20 mg |
| Cmax | 0.25 - 20 ng/mL |
| Tmax | 30 - 360 minutes (0.5 - 6 hours) |

### Standard Immediate-Release Minoxidil PK (Published Literature)

From published pharmacokinetic studies (Fleishaker et al., J Clin Pharmacol 1989; PMC10806356):

| Parameter | IR Minoxidil 2.5mg | Veradermics Claimed Range | Falls Within Claims? |
| --- | --- | --- | --- |
| Cmax | 16.8 ± 7.83 ng/mL | 0.25 - 20 ng/mL | YES |
| Tmax | 1 hour (60 min) | 30 - 360 minutes | YES |

Standard immediate-release minoxidil ALREADY achieves the PK parameters claimed in the patent.

### Implications for Patent Validity

This creates potential invalidity arguments under 35 U.S.C.:

- Lack of Novelty (§102): If IR minoxidil was used to treat hair loss before October 2022 (Veradermics’ priority date) and achieved these PK parameters, the claims may be anticipated by prior art.

- Obviousness (§103): It may have been obvious to administer minoxidil at doses achieving these PK parameters for hair loss treatment, given the extensive off-label use of oral minoxidil for alopecia.

- Indefiniteness (§112): The claims are so broad they would cover existing IR minoxidil use, suggesting the claims may not particularly point out and distinctly claim the invention.

### Prior Art: Off-Label Oral Minoxidil for Hair Loss

Oral minoxidil (Loniten®) has been used off-label for hair loss treatment for years: - Multiple published case series and studies prior to 2022 - Doses ranging from 0.25mg to 5mg daily - Known PK profile achieving Cmax ~17 ng/mL at 2.5mg

### Strategic Implications

- For Invalidity Challenge: This analysis suggests Veradermics’ patent claims may be vulnerable to an invalidity challenge based on anticipation or obviousness.

- For Freedom-to-Operate: Even if our formulations technically achieve the claimed PK parameters, we may have a strong invalidity defense.

- For IPR/PGR: Consider filing an Inter Partes Review (IPR) or Post-Grant Review (PGR) to challenge the patent claims based on this prior art.

### Recommended Action

Engage patent counsel to: 1. Conduct prior art search for publications on oral minoxidil PK for hair loss pre-dating October 2022 2. Evaluate strength of invalidity arguments 3. Consider IPR/PGR petition to narrow or invalidate overly broad claims

## Important Caveats

- Patent freedom-to-operate analysis required - Have IP attorney review all formulations against full Veradermics claim set

- Formulation optimization needed - These are starting points requiring systematic development

- In vitro-in vivo correlation (IVIVC) - Establish relationship between dissolution and absorption

- Clinical PK studies - Required to confirm target profile achieved

- CMC development - Full pharmaceutical development and validation required

- IND required - Any human testing requires FDA IND approval

## References

- Osmotic Pump Drug Delivery Systems - PMC (PMID: 36407821)

- Ethylcellulose/Eudragit Coating Systems - PMC (PMID: 27478784)

- Compritol 888 ATO Monograph - Gattefosse

- Cellulose Acetate Membranes for Osmotic Systems - PubMed (PMID: 12056533)

- Minoxidil Physicochemical Properties - PubChem CID 4201

- Veradermics Patent WO2024091572A1 - Google Patents

- Veradermics Patent US12268688B2 - USPTO

Document prepared for competitive intelligence and product development purposes. Not legal advice. Consult patent attorney before proceeding with development.